DSC curves of the alloy #1

350                                                   400        T,K

HEATING

0,1 J/(g·K)

Fig.1.a. Samples after quenching and aging during 30 min at 130C .

COOLING

350                                                    400     T,K

0,1 J/(g·K)

HEATING

Fig.1.b. Thermocycle 1.